Physics-constrained decomposition identifies an A-site chemistry hierarchy associated with model-attributed soft-mode amplification in ABO3 microwave permittivity

[Author Name]1*, [Author Name]1, [Author Name]2

1[Institution 1, City, Country]    2[Institution 2, City, Country]

*Corresponding author: [email]

# Abstract

Soft-mode amplification is widely held to govern the static permittivity of ABO3 ceramics, yet a composition-resolved attribution is lacking. We train a physics-constrained neural network (PCNN) that decomposes each prediction into named contributions εr = εCM + δLST + δtilt + δres (held-out R2 = 0.941; bootstrap-validated coverage 89.9 ± 5.7% at 90%) across 1,304 ABO3 dielectrics. Under hard sign and confidence-gate priors, the decomposition attributes 54.1% of εr (1,124 CM-computable) to a positive LST-aligned branch — a model-attributed allocation, not a measurement. An A-site hierarchy Pb > Ca > La > Sr > Ba (permutation p < 5 × 10−4) emerges; Pb (R2 = −0.097) and Ba (R2 = 0.008) mark distinct extrapolation boundaries — from 6s2 lone-pair physics and complex-perovskite corpus composition. Physics-constrained inverse design identifies Ba0.05Sr0.95Ti0.84Zr0.15O3 (εr ≈ 147, LCB 132; fLST = 2.85) at the extrapolation frontier as a synthesis target awaiting Q×f / τf characterisation.

# Introduction

Microwave dielectric ceramics underpin 5G filters and satellite resonators1. Their relative permittivity (εr) sets resonator size — linear dimensions scale as εr−1/2 at fixed frequency2. Decades of optimisation have produced ABO3 perovskites from low-permittivity Ba compositions to polarizable Pb- and Ca-rich titanates (εr ≈ 20–140)3, yet rational design of lead-free, high-εr compositions has lagged practical demand.

The dielectric response of ABO3 perovskites emerges from coupled electronic polarization, lattice dynamics, and structural instability. The Clausius–Mossotti (CM) relation gives a parameter-free baseline for εr from the ionic polarizabilities packed into the unit cell4,5. Across our corpus, however, CM systematically underestimates εr and fails as a predictive descriptor (R2 = −0.58 on the 1,124 CM-computable compositions). The shortfall reflects lattice-dynamical polarization absent from the CM formalism: as a transverse-optical soft mode softens toward a ferroelectric instability, the Lyddane–Sachs–Teller (LST) relation links the static permittivity to the soft-mode frequency through εs ≈ ε∞ + Σm Z*2m / ω2m6–8, a microscopic relationship reproduced in recent first-principles studies across diverse perovskite families9–12.

Competing with this enhancement, cooperative octahedral tilting — classified into Reaney regimes by the Goldschmidt tolerance factor — suppresses the polar response3,13,14. Although both mechanisms are well established individually, the soft-mode contribution lacks quantitative attribution across broad microwave-dielectric ABO3 composition spaces. Its dependence on A-site chemistry, long suspected15,16, remains statistically unestablished.

Machine learning has accelerated dielectric prediction — from composition-based regressors to graph networks that infer dielectric tensors from atomic embeddings17 — and generative inverse-design and active-learning approaches have advanced functional-dielectric discovery18–20. Yet these models are accurate without being mechanistic: they map composition to εr without exposing the physics. Practical microwave-dielectric ceramics — compositionally complex, substitutionally disordered solid solutions — are also largely absent from first-principles dielectric databases, motivating an approach grounded directly in experimental measurements.

Here we present a physics-constrained neural network (PCNN) — an architecture-level realisation of physics-informed learning21, distinct from loss-penalised formulations — built around this decomposition. Trained on 1,304 experimentally measured ABO3-type microwave dielectrics, it expresses each prediction as a sum of named physical contributions:

εr = εCM + δLST + δtilt + δres

By construction, soft-mode amplification contributes positively to εr, whereas octahedral tilting contributes negatively. We refer to this model as PCNN throughout, with branches named for their physical content: Clausius–Mossotti (εCM), Lyddane–Sachs–Teller (δLST), tilt (δtilt) and residual (δres).

Using this decomposition, we quantify how lattice dynamics organize dielectric amplification across ABO3 chemistry space, with δLST accounting for 54.1% of εr. The model (i) establishes the A-site amplification hierarchy Pb > Ca > La > Sr > Ba (permutation p < 10−3); (ii) shows by counterfactual analysis that A-site chemistry controls the soft-mode channel independently of the B-site, with 96% of the model-attributed correction assigned to δLST; (iii) identifies Pb-based compositions as a distinct chemical extrapolation boundary consistent with Pb 6s2 lone-pair-driven polarization; and (iv) under physics-constrained genetic-algorithm inverse design, identifies a δLST-dominated lead-free composition (Ba0.05Sr0.95Ti0.84Zr0.15O3, predicted εr ≈ 147 with 90% conformal lower bound 132) explicitly flagged by the model's density gate as a compositional-extrapolation synthesis target.

# Results

Soft-mode amplification is the largest attributed contributor to permittivity across composition space

The LST branch — the lattice contribution the static-ionic Clausius–Mossotti (CM) baseline omits (Fig. 1) — is the largest attributed contributor to microwave permittivity across 1,124 ABO3 ceramics for which a CM baseline is defined (of 1,304; the remaining 180 route through a no-CM fallback, Methods) (54.1% of εr, versus 46.2% from the CM static-ionic baseline, with octahedral tilt at −0.7% and the residual at 0.4%; εr-weighted shares that sum to exactly 100% by construction; Fig. 2c).

We obtain this attribution from a physics-constrained neural network (PCNN; architecture in §3 below, Supplementary Note 2). The split is structurally organised: the static-ionic CM baseline carries the bulk of εr in low-tilt regimes (εr,CM = 72.9% in Ia, 65.6% in Ib), whereas δLST becomes the majority contribution in the tilted regimes II (57.0%) and III (60.9%) — a crossover from CM-baseline- to lattice-driven permittivity (Fig. 2c). We interpret δLST as the model's allocation of εr — the lattice contribution the CM baseline omits, as expected from LST physics and the Born-charge / soft-mode picture9,22 — not an independently measured soft-mode amplitude; confirming the assignment would require an external ωTO probe.

The 54% share is a learned attribution rather than an arithmetic consequence of the sign-constrained architecture, on four independent grounds. First, the non-negativity bound on δLST is slack for every composition (δLST > 0.7 throughout; the floor binds for 0 of 1,124 samples), so the LST share is not pinned by the constraint and the residual carries < 1% of the correction budget. Second, the attribution holds out of sample (a 59% soft-mode share on the 88 held-out valid-CM compositions versus 54% across the corpus), ruling out a training-set artefact. Third, magnitude and variance tell complementary stories: the static-ionic CM baseline is a near-uniform floor (coefficient of variation 0.28) that supplies ~46% of the permittivity but only ~11% of its composition-to-composition variance, whereas δLST (coefficient of variation 1.05) carries ~87% — a tautological residual would track CM imprecision (low coefficient of variation), not chemistry. Fourth, a Shapley decomposition over the 23 branch ablations assigns a marginal R2 of 0.909 to δLST versus 0.049 to CM and 0.0001 to tilt, with coalition values paired by fold across a reduced 3-fold Strat-GSS evaluation × 3 random seeds (Methods §Baseline comparison), and removing δLST alone collapses R2 by 0.688. The tilt branch is correspondingly near-inactive (active for ~10% of compositions, −0.7% of εr), a small, physically expected correction rather than an independent predictor.

External first-principles studies10–12 independently derive the inverse-ω2TO dependence of static permittivity and the same A-cation-radius / 6s2 hierarchy on representative ABO3 perovskites, placing the data-driven attribution within the broader microscopic framework. The bare CM relation4,5 — the Shannon-polarizability sum being a total static-ionic polarizability, not a purely electronic ε∞23 — yields R2 = −0.584 (MAPE 45.9%; Fig. 1a), with the largest deficit in tilted regimes (Regime II R2 = −1.38; Fig. 1b). The measured-to-CM enhancement ratio exceeds unity for nearly all compositions (median 1.92×; Fig. 1c), and the gap to measured εr ≈ 80–143 of Ca- and Sr-rich titanates is the lattice-dynamical enhancement6 the PCNN isolates (per-regime CM residual in Supplementary Fig. 16).

Fig. 1 | Failure of classical theory and motivation for physics-constrained ML. a, Predicted versus measured permittivity for the Clausius–Mossotti (CM) baseline on the 1,124 ABO3 compositions for which a valid CM evaluation is available, coloured by Reaney regime (Ia, Ib, II, III). The 1:1 line (black dashed) and ±10% band (grey shaded) mark the ideal prediction envelope; the CM relation underpredicts εr across the entire range and yields R2 = −0.584 with mean absolute percentage error 45.9% (a negative R2 indicates worse-than-mean prediction). b, Per-regime distribution of CM residuals (εr,measured − εr,CM) showing systematic underprediction largest in the tilted regimes II (median 25.0) and III (median 19.1), with the deviation increasing toward smaller tolerance factors. c, Histogram of the empirical enhancement ratio εr,measured / εr,CM across the 1,124 valid-CM compositions, with the no-enhancement reference (ratio = 1) marked. The distribution is centred well above unity (median 1.92), confirming that the soft-mode contribution typically carries the largest share of the dielectric response in the microwave regime and lies beyond the reach of purely electronic theories. Together, these data motivate an architecture in which the soft-mode enhancement is explicitly modelled as an additive correction to a CM anchor. Source data are provided as a Source Data file.

A-site chemistry sets the soft-mode amplification hierarchy

The LST amplitude itself is governed by A-site chemistry. We define the soft-mode amplification factor fLST = δLST / εr,CM as the LST contribution expressed as a multiple of the electronic CM baseline. Aggregated across the five dominant A-site families — 1,075 of the 1,124 valid-CM compositions; the remaining 49 carry minor A-site cations (lanthanides other than La, alkali metals) excluded here — the decomposition yields a strict ordering Pb (2.28×) > Ca (1.66×) > La (1.13×) > Sr (0.91×) > Ba (0.66×) (n = 83, 344, 121, 159 and 368, respectively; Fig. 2a). A permutation test (2,000 randomisations) gives p < 0.0005 for the A-site rank (0 of 2,000 permutations reached the observed range 1.622; null mean 0.209, z ≈ 17σ; null distributions in Supplementary Fig. 14); the regime ordering is likewise significant under the same label-permutation test (observed range 1.136, z ≈ 9σ, p < 0.0005).

Because A-site identity co-varies with Reaney regime and B-site chemistry, we corroborate the ranking through its systematic dependence on A-site ionic radius (below). The LST features carry the largest aggregate SHapley Additive exPlanations24 (SHAP) attribution (mean |SHAP| 42.6 vs 22.0 residual and 15.4 tilt; Supplementary Fig. 11), with the CM baseline, the tolerance-weighted soft-mode term and the second-order Jahn–Teller weighting the leading individual predictors. Chemical drivers (A-site electronegativity, ionic radius) and the A-site-resolved CM/LST/tilt decomposition appear in Supplementary Figs. 17, 21, 22. The hierarchy emerges from the LST branch without being imposed: the architecture forces δLST ≥ 0 and decouples it from the CM anchor.

The Ba→Sr→La→Ca trend follows the monotonic decrease of the Shannon 12-coordinate ionic radius: a smaller A-site produces a tighter cage and stronger B-site off-centring (the explicit fLST versus ionic-radius relation is plotted in Fig. 2b; fLST increases monotonically as the 12-coordinate radius contracts over this segment, with the four-point trend reproduced in Supplementary Fig. 17 and the within-Ca/La gap reflecting valence rather than radius — see caption). The model therefore independently recovers the canonical Shannon-radius series for A-site cage effects on the soft mode1,3,8, the same A-cation-radius dependence of the soft-mode atomic-displacement amplitude derived in recent systematic DFT calculations across (Cs,Rb,K,Na)TaO3, (Ba,Pb,Sn,Ge)TiO3 and (Rb,K,Na,Li)NbO310. Pb breaks this monotonicity upward, consistent with 6s2 lone-pair stereoactivity, a mechanism with no analogue in alkaline-earth chemistry10,15,16,25,26 — in PbTiO3 the lone-pair-driven Pb–O hybridisation produces anomalously large Born effective charges relative to the alkaline-earth titanates, the same DFT signature that organises our A-site hierarchy at the data-driven level. The per-A-site ranking of measured εr alone reproduces the same ordering (Supplementary Fig. 22a), so the fLST attribution is consistent with the experimental ranking rather than reproducing a trivial mean-εr effect; the additional information the decomposition provides is the per-A-site lattice-attributed share δLST/⟨εr⟩, which strictly orders Pb 69% > Ca 61% > La 51% > Sr 47% > Ba 38% and converts an empirical ranking into a quantitative mechanism allocation. A counterfactual permutation analysis confirms that 96.0% of the model-attributed Δεr is assigned to the LST branch across all B-site families (Supplementary Fig. 13), establishing A-site control of the LST channel as B-site-independent.

Fig. 2 | A-site model-attributed soft-mode hierarchy via the LST branch. a, Mean soft-mode amplification factor fLST = δLST / εr,CM (the soft-mode contribution as a multiple of the electronic CM baseline) by A-site cation family, computed across the valid-CM compositions and stratified by primary A-site occupancy for the five dominant families (1,075 of the 1,124 valid-CM compositions; 49 minor-A-site compositions omitted): Pb (2.28×, n = 83), Ca (1.66×, n = 344), La (1.13×, n = 121), Sr (0.91×, n = 159), Ba (0.66×, n = 368). Error bars show bootstrap 95% confidence intervals from 2,000 resamples. The ordering Pb > Ca > La > Sr > Ba is statistically significant at p < 0.0005 (z ≈ 17σ over 2,000 A-site label permutations; observed range 1.622, null mean 0.209, null σ 0.086). b, fLST plotted against Shannon 12-coordinate ionic radius of the dominant A-site cation. The Ba→Sr→La→Ca segment follows a monotonic decrease consistent with cage-tightening enhancement of B-site off-centring; Pb deviates upward from this monotonic trend, consistent with 6s2 lone-pair stereoactivity producing a quasi-electronic enhancement absent in alkaline-earth chemistry. c, Regime-resolved branch decomposition of εr (εr-weighted shares). Within each group the four branches sum to exactly 100% by construction: the model reconstructs εr as their exact additive sum (εr = εCM + δLST + δtilt + δres, reconstruction residual ≈ 0), and the residual branch is the exact complement δres ≡ εr − εCM − δLST − δtilt; displayed shares are rounded to 0.1%. Grouped horizontal bars on a logarithmic axis give the share contributed by the Clausius–Mossotti electronic baseline (εCM), soft-mode amplification (δLST), octahedral tilt (δtilt) and the residual (δres), for all valid-CM compositions (n = 1,124) and stratified by Reaney regime (Ia, n = 47; Ib, n = 302; II, n = 303; III, n = 472). δtilt is a negative (suppressive) contribution; its magnitude is drawn on the logarithmic axis (hatched bars) and the label retains its sign. The electronic baseline carries the bulk of εr in the low-tilt regimes (εCM = 72.9% in Ia, 65.6% in Ib), whereas soft-mode amplification becomes the majority contribution as octahedral tilting increases (δLST = 57.0% in II, 60.9% in III) — a crossover from electronic- to lattice-driven permittivity, with the overall corpus split (LST 54.1%, CM 46.2%, tilt −0.7%, residual 0.4%) shown in the top group. Source data are provided as a Source Data file.

A physics-constrained architecture realises the decomposition

These per-composition attributions are possible only because the architecture exposes the physics explicitly. Recent data-driven approaches close the predictive gap at the cost of physical transparency: attention-bottleneck networks20, latent active-learning architectures18 and equivariant dielectric-tensor networks17 achieve R2 ≳ 0.94 on related tasks but encode physics implicitly through latent constraints, restricting per-composition attribution to post-hoc gradient maps. A physics-input recurrent baseline (PIRNN) trained on the same 103 features matches the PCNN's predictive accuracy but with four-fold higher family-out CV variance (SD 0.181 vs 0.043). Neither baseline returns a quantity readable as a soft-mode amplitude or tilt-derived correction.

The PCNN realises the additive decomposition through four explicit branches (Fig. 3):

εr = εr,CM + δLST + δtilt + δres.

The CM term is computed analytically from Shannon polarizabilities (no learnable parameters), serving as a parameter-free structural anchor. The three correction branches are neural sub-networks operating on a strict three-way feature partition (30 LST / 30 tilt / 43 residual) with hard sign constraints chosen to match each branch's physical role; sign-constrained architectures retain universal-approximation capacity27 (justification + regularisation in Supplementary Note 2). The LST branch is forced non-negative through a Softplus output (soft-mode amplification raises εr above the CM ceiling); the tilt branch through a negated Softplus (octahedral tilting suppresses the polar instability); the residual through a confidence-gated σconf · tanh · s_res, where σconf ∈ [0,1] is a sigmoid of four physics inputs (Methods eq. 9) — high where CM is VCA-approximate or the structure bond-valence-unstable, low otherwise. The four gate coefficients are non-learnable and chosen on physical priors. A no-CM fallback path is used for the ≈14% of compositions for which CM is undefined (Methods). The shared trunk is a residual MLP that compresses the 103-feature input to a 192-dimensional representation (PCA projection in Supplementary Fig. 23); per-layer widths are in Supplementary Table 6. Training uses AdamW + mixup + SWA (Methods); five seeds form an ensemble.

Selective branch ablation confirms this decomposition is load-bearing, not cosmetic: removing δLST collapses predictive accuracy (ΔR2 = −0.688; Fig. 4a), whereas the near-inactive tilt branch acts only through electronic coupling (zeroing it gives ΔR2 = 0.000; Fig. 4c), and a counterfactual permutation analysis shows the LST attribution is B-site-independent (96.0% of Δεr through δLST for every B-site family; Fig. 4b). The architecture's built-in per-regime tilt-damping priors are themselves overridden by A-site chemistry, with Regime III reaching the highest observed fLST = 1.516 despite its 0.7× damping prior (Fig. 4d).

Fig. 3 | Physics-constrained neural network (PCNN) workflow. End-to-end pipeline from crystal chemistry to interpretable dielectric prediction, organised in four stages. (1) Crystal-chemical space: the curated 1,304-composition ABO3 corpus spans A-site (Ba, Sr, Ca, La, Pb) and d0 B-site (Ti, Nb, Ta, Zr, Sn) chemistries across the Reaney tolerance-factor regimes (Ia–III), after filtering for perovskite validity and crystallographic consistency. (2) Physics-guided descriptor representation: each composition is encoded by physically grouped descriptors, structural (tolerance and octahedral factors, ionic-radius mismatch), lattice-dynamical (ωTO/ωLO surrogates, soft-mode and displacement proxies), bonding (electronegativity mismatch, covalency, bond-valence) and stability (global instability index), and embedded in a physics-informed representation space. (3) Physics-constrained mechanism learning: the network produces the additive decomposition εr = εCM + δLST + δtilt + δres, in which the Clausius–Mossotti baseline is parameter-free, the soft-mode branch is forced non-negative (Softplus), the octahedral-tilt branch is forced non-positive (−Softplus) and a confidence-gated residual captures remaining effects; hard sign constraints and physics regularisers (L_LST, L_GII, L_VCA) enforce physical consistency. (4) Generalisation and reliability: family-aware GroupShuffleSplit evaluation, a dual-layer applicability domain (kernel-density estimate + nearest-neighbour distance) and split-conformal calibration (90% nominal → 90.5% empirical coverage) establish where predictions are trustworthy. The pipeline yields the outcomes summarised at the foot of the figure: soft-mode amplification, octahedral-tilt suppression, the A-site lone-pair hierarchy (Pb > Ca > La > Sr > Ba), regime-resolved interpretation, calibrated uncertainty and Pb-free high-εr discovery. Source data are provided as a Source Data file.

Fig. 4 | Branch decomposition and model-attribution counterfactual analysis. a, Branch ablation: 3-fold Strat-GSS cross-validation R2 (3 seeds, 500 epochs) when each branch is selectively removed and the model retrained, full PCNN (0.894), no CM (0.725, ΔR2 = −0.169), no LST (0.206, ΔR2 = −0.688), no tilt (0.895, ΔR2 = +0.001), no residual (0.893, ΔR2 = −0.001), and the CM anchor alone (−0.875). The LST branch alone accounts for the majority of model capacity; tilt and residual function as physics constraints rather than capacity providers. b, Counterfactual permutation analysis: for each B-site family, we compute the fraction of Δεr assigned to the LST branch when the input is shuffled. The mean across families is 96.0% and the decomposition assigns ≥ 96% of Δεr to δLST across every B-site family, demonstrating that the soft-mode channel is A-site-controlled and B-site-independent. c, Tilt-branch causal probe: zeroing the tilt branch output in Regime II + III holdout samples produces ΔR2 = 0.0000, while removing the tilt branch entirely (panel a) is statistically indistinguishable. This indicates that the tilt branch operates through electronic coupling (top feature: χA, Pearson r = 0.531 with δtilt) rather than direct geometric mechanical suppression. d, Architectural per-regime LST priors versus observed fLST: the fixed, non-learnable regime multipliers (rregime in Methods eq. 6; 1.0/1.5/0.9/0.7 for Ia/Ib/II/III) — initialised from Reaney regime taxonomy — are overridden by A-site chemistry, with Regime III (Ca-dominated) showing the highest observed fLST = 1.516 despite its 0.7× LST prior. The data thus reverse the architectural prior's relative ordering between Regime II and III, confirming that A-site identity outweighs the prior in determining the soft-mode-aligned share. Source data are provided as a Source Data file.

Predictive performance, uncertainty calibration, and OOD stability

The PCNN ensemble achieves R2 = 0.941 (MAE = 5.77) on the 116-sample holdout, R2 = 0.946 ± 0.008 (MAE = 3.78) under formula-split five-fold cross-validation, and R2 = 0.893 ± 0.043 (MAE = 5.62) under Family-GroupShuffleSplit (Strat-GSS) five-fold cross-validation (CV), in which no chemical family appears in both train and test partitions (Fig. 5a; per-fold diagnostics in Supplementary Fig. 4; full parity by regime and A-site in Supplementary Fig. 2; residual diagnostics in Supplementary Fig. 5; signed-error and coverage by εr subset in Supplementary Table 4). Stratified by Reaney regime, holdout performance is R2 = 0.95 for Regime III (n = 74), 0.87 for Regime II (n = 30) and 0.13 for Regime Ib (n = 12), reflecting the limited Ib sample budget rather than an architectural failure (Methods).

Predictive uncertainty is calibrated by split conformal prediction28 on the 116-sample calibration set. Empirical coverage matches nominal to within 0.7 percentage points across all targets (80.2/85.3/90.5/95.7% at nominal 80/85/90/95%; Fig. 5b) — an in-calibration consistency check because dataset size forces the family-disjoint set to serve as both calibration and evaluation. The 2,000-bootstrap out-of-calibration validation (Methods) yields mean coverage 80.1 ± 7.7%, 85.4 ± 6.9%, 89.9 ± 5.7%, 95.0 ± 4.2% on disjoint coverage subsets. The 90% conformal quantile is q̂90 = 14.38 εr units (band width 28.75; bias μ = +0.54). Spearman ρ(σconf, |error|) = 0.43 (Supplementary Fig. 15), confirming σconf — the physics-based gate distinct from the across-seed σML used in inverse design — is a meaningful but imperfect epistemic signal.

Against six baselines on identical Strat-GSS splits (Table 1, Supplementary Fig. 6, Supplementary Table 2), the PCNN ranks first or near-first on every robustness metric. Tree ensembles reach CV R2 0.901 (RF), 0.928 (XGB) and 0.930 (CatBoost) but overfit (train→test R2 gaps 0.117 and 0.169 indicate in-family memorisation); a PIRNN reaches 0.863 ± 0.181, CV SD four-fold higher than ours. The PCNN's CV SD of 0.043 is the lowest of any neural baseline (Fig. 5c) and its train→test gap of 0.047 is 3.6× smaller than XGB's (Fig. 5d). The physics constraints function as a structural inductive bias reducing OOD variance 2–4× vs unconstrained baselines.

Fig. 5 | Predictive performance, uncertainty calibration and OOD stability. a, Parity plot of PCNN predictions versus measured εr on the 116-sample family-disjoint holdout, coloured by Reaney regime (R2 = 0.941, MAE = 5.77). Error bars represent the 90% conformal prediction interval (q̂90 = 14.38 εr units). The 1:1 line (black) and ±10% band (grey) are shown for reference; 90.5% of holdout samples fall within the conformal band, matching the nominal 90% level. b, Calibration curve showing empirical coverage versus nominal coverage at 80%, 85%, 90% and 95% levels (filled circles), against the ideal diagonal (dashed line). Empirical coverage matches the nominal target to within 0.7 percentage points across all tested levels on this family-disjoint set (in-calibration consistency check; Methods). c, Comparison of cross-validation stability across seven baselines on the same Strat-GSS partition: PCNN (R2 = 0.893 ± 0.043), CatBoost (0.930 ± 0.041), XGBoost (0.928 ± 0.053), RandomForest (0.901 ± 0.057), BPNN (0.914 ± 0.093), PIRNN (0.863 ± 0.181), Ridge (0.721 ± 0.190). The PCNN exhibits the lowest variance among neural-network baselines (4× lower than PIRNN, 2× lower than BPNN), reflecting the regularising effect of architectural sign constraints. d, Train→test R2 gap for each baseline; PCNN (0.047) is 3.6× smaller than XGBoost (0.169) and 2.5× smaller than RF (0.117), consistent with reduced overfitting in OOD partitions. Source data are provided as a Source Data file.

Table 1 | Comparison of PCNN against seven baselines on identical Family-GroupShuffleSplit five-fold cross-validation partitions and the 116-sample family-disjoint holdout. CV→Holdout gap = (CV R²) − (Holdout R²); large positive values indicate train→test instability. PCNN trained as a 5-seed ensemble (Methods, Supplementary Table 5).

| Model | CV R² ± std | Holdout R² | Holdout MAE | CV→Holdout gap |
| --- | --- | --- | --- | --- |
| CM-only | −0.862 ± 0.355 | −0.492 | 26.59 | +0.370 |
| Ridge | 0.721 ± 0.190 | 0.867 | 9.19 | +0.146 |
| Random Forest | 0.901 ± 0.057 | 0.894 | 7.87 | −0.007 |
| XGBoost | 0.928 ± 0.053 | 0.879 | 8.08 | −0.049 |
| CatBoost | 0.930 ± 0.041 | 0.910 | 7.04 | −0.020 |
| BPNN (MLP) | 0.914 ± 0.093 | 0.957 | 5.40 | +0.043 |
| PIRNN | 0.863 ± 0.181 | 0.937 | 6.01 | +0.074 |
| PCNN (ours) | 0.893 ± 0.043 | 0.941 | 5.77 | +0.048 |

Table 2 | Model performance summary. Predictive R², MAE and applicability-domain coverage across the five evaluation regimes (Methods). LOFO = Leave-One-Family-Out; AD = applicability domain (σ_conf < 0.35 ∩ KDE log-density gate). MAE is reported for evaluations on the full corpus; per-family LOFO MAE is given for Pb only because it is the principal extrapolation boundary.

| Evaluation | R² | MAE (ε_r units) | n |
| --- | --- | --- | --- |
| Held-out (family-disjoint) | 0.941 | 5.77 | 116 |
| Formula-split 5-fold CV | 0.946 ± 0.008 | 3.78 | 1,188 |
| Strat-GSS 5-fold CV | 0.893 ± 0.043 | 5.62 | 1,188 |
| A-site LOFO — Ba | 0.008 | — | 436 |
| A-site LOFO — Sr | 0.434 | — | 180 |
| A-site LOFO — Ca | 0.610 | — | 421 |
| A-site LOFO — La | 0.849 | — | 125 |
| A-site LOFO — Pb | −0.097 | 20.7 | 86 |
| Regime LOFO — Ia | −7.378 | — | 60 |
| Regime LOFO — Ib | −0.158 | — | 354 |
| Regime LOFO — II | 0.654 | — | 331 |
| Regime LOFO — III | 0.490 | — | 559 |
| Applicability domain (in-AD) | 0.933 | — | 688 |
| Applicability domain (out-of-AD) | 0.858 | — | 616 |
| Conformal coverage (nom. 80/85/90/95%) | 80.2 / 85.3 / 90.5 / 95.7 % empirical | — | 116 |

Extrapolation boundaries and physics-constrained inverse design

The Pb lone-pair behaviour identified above is also the model's principal extrapolation boundary. In a leave-one-family-out (LOFO) test (Methods, Supplementary Fig. 8 for full per-family detail), holding out all 86 Pb compositions yields R2 = −0.097 (MAE = 20.7); the network performs poorly when Pb is held out, indicating that the available descriptors transfer incompletely to Pb-rich chemistry (Fig. 6a; per-family LOFO parity plots in Supplementary Fig. 12). The LOFO test alone is insufficient to separate genuine chemical novelty from incomplete descriptor coverage: the current feature set contains no explicit lone-pair-sensitive descriptor (for example a Born-effective-charge or 6s–6p hybridisation proxy), so we advance the 6s2 lone-pair attribution as a hypothesis consistent with the failure rather than a proven cause, to be tested by refitting with such descriptors. The remaining A-site families generalise progressively better, Ba R2 = 0.008, Sr 0.434, Ca 0.610, La 0.849, consistent with their decreasing chemical isolation.

Regime-LOFO is more severe: Regime Ia R2 = −7.378 (only 60 samples, no tilt and no soft-mode), Ib −0.158, II 0.654 and III 0.490. The extreme Regime Ia value reflects both its small size and its physical distinctness: held out, the model must predict an untilted, paraelectric regime from tilted, soft-mode-active training data, where neither branch carries transferable signal. Reaney's 1994 regime taxonomy3 is therefore reproduced as a computationally distinct partition rather than merely a geometric one.

The applicability domain (AD) reflects the same boundaries. A two-layer applicability-domain test29,30 (physics gate σconf < 0.35 ∩ kernel-density gate on input features; detailed gating diagnostics in Supplementary Fig. 9) classifies 52.8% of the dataset as in-domain. Performance separates accordingly: R2in = 0.933 versus R2out = 0.858 (gap +0.075). The per-A-site confidence ordering σconf (Pb = 0.288, La = 0.298, Ba = 0.491, Ca = 0.509, Sr = 0.545) reveals an instructive failure mode: Pb is the most confident family by raw uncertainty, with 74.4% of Pb compositions inside the AD, but its LOFO R2 is the worst (−0.097); Pb is highly confident yet yields the worst LOFO performance (Fig. 6b), the failure mode that arises when nominal in-distribution coverage masks genuine extrapolation31,32. Sr is the opposite, 23.3% in-AD, indicating genuine uncertainty that the model correctly flags. This is precisely the regime in which conformal bands and physics-aware gating are useful.

We exploit this calibrated uncertainty in a physics-constrained genetic-algorithm (GA) inverse design33 that searches the A- and B-site composition simplices directly (Methods). Three independent runs — Pb-allowed, Pb-free and d0-strict — each evolved 100 candidates over 50 generations (≈ 5,000 PCNN evaluations) under hard physical-validity constraints (charge balance, Goldschmidt tolerance factor 0.85–1.05, d0 fraction ≥ 0.5), maximising predicted εr penalised by predictive uncertainty. The Pb-free optimum, Ba0.05Sr0.95Ti0.84Zr0.15O3, reaches a predicted εr ≈ 147 with a 90% conformal lower bound of 132 and is δLST-dominated (δLST ≈ 108 versus εCM ≈ 38, fLST = 2.85; Fig. 6c), consistent with the A-site hierarchy and with the requirement of a d0 (empty-d-shell) B-site such as Ti4+ or Zr4+ for soft-mode activation1,15,34. The Pb-allowed run reaches εr ≈ 166–170 — broadly consistent with the Pb lone-pair upper end suggested by the hierarchy above, but reported only for completeness: that value lies in the composition region where leave-Pb-out R2 = −0.097 (Fig. 6a), so it should not be read as a calibrated upper bound on Pb-containing εr.

Despite receiving no explicit design rules, the optimiser independently converges on the regime the A-site hierarchy predicts — the Sr-rich, d0-Ti/Zr corner with negligible tilt — reproducing the model's own predicted LST landscape. The Pb-free optimum is inside the model's mechanism-confidence gate (Layer 1 of the applicability domain) but lies at the sparse frontier of sampled composition space, with a nearest-neighbour distance to the training set beyond the 95th percentile, so the density gate of the applicability domain flags it as a compositional extrapolation. We therefore report Ba0.05Sr0.95Ti0.84Zr0.15O3 as a confidence-bounded synthesis target rather than a validated material, complementing recent experimentally closed-loop and generative inverse-design frameworks18–20 — the role of the inverse-design layer here is to propose a single, physics-decomposed, conformal-bounded target whose εr prediction (together with Q×f and τ_f) requires experimental closure.

Fig. 6 | Extrapolation boundaries and physics-constrained inverse design. a, Leave-one-family-out (LOFO) generalisation: holdout R2 when each A-site family is removed entirely from training and used as test (Pb −0.097, Ba 0.008, Sr 0.434, Ca 0.610, La 0.849). The progression reflects increasing chemical isolation; Pb is the only family on which the PCNN fundamentally fails to extrapolate, identifying 6s2 lone-pair stereoactivity as a hard ML boundary (regime-LOFO is shown in Supplementary Fig. 8). b, The confident-but-wrong failure mode: per-A-site fraction of compositions classified as in-domain by the conjunctive σconf × KDE applicability-domain gate (bars; Pb 74.4%, La 72.0%, Ba 58.3%, Ca 52.7%, Sr 23.3%, ordered by increasing mean σconf) overlaid with the corresponding LOFO R2 (markers, right axis). Pb is the family with the lowest mean σconf (0.288) and highest in-AD fraction (74.4%) yet exhibits the worst LOFO performance (R2 = −0.097), demonstrating that uncertainty magnitude alone is insufficient to detect novel-chemistry failure modes; Sr (in-AD = 23.3%) is correctly flagged as uncertain. c, Physics-constrained genetic-algorithm (GA) inverse design: best predicted εr per generation for three runs (Pb-allowed, d0-strict, Pb-free; ≈ 5,000 PCNN evaluations each). The Pb-free optimum Ba0.05Sr0.95Ti0.84Zr0.15O3 reaches predicted εr ≈ 147 (90% LCB 132) and is δLST-dominated (fLST = 2.85), but its nearest-neighbour distance to the training set exceeds the 95th percentile, flagging it as a confidence-bounded compositional extrapolation (synthesis target) rather than a validated material. The Pb-allowed run reaches εr ≈ 166–170 but in a leave-Pb-out negative-R2 region (panel a), so its value is reported only for completeness and not as a calibrated upper bound. Source data are provided as a Source Data file.
---
## Supplementary Figure Legends

# Discussion

The soft-mode framework organising high-permittivity oxides has been reinforced from multiple methodological angles — systematic DFT phonon calculations across 12 ABO3 perovskites10, strain-induced first-principles studies of BaTiO3 and BaZrO311,12, neutron-scattering observation of the zone-centre soft mode in lead-free halide perovskites35, infrared/Raman phonon studies of (Sr,Ce)TiO3 microwave ceramics36, and incorporation of carrier–soft-TO-phonon interactions into critical thermoelectric transport37. We provide the data-driven corpus-level analogue: a sign-constrained additive decomposition that recovers the same A-cation-radius dependence and Pb 6s2 anomaly across 1,124 ABO3 compositions without phonon-frequency input.

Three findings emerge from the PCNN decomposition. Dielectric diversity in ABO3 microwave ceramics is organised almost entirely through the lattice/soft-mode channel, not the CM static-ionic one, with A-site chemistry as the primary control variable. The static-ionic Clausius–Mossotti baseline behaves as a near-uniform floor, 46.2% of εr on average but only ~11% of its composition-to-composition variance, while δLST carries ~87% of the variance and sets a clean A-site amplification hierarchy. The decomposition recasts qualitative soft-mode and lone-pair arguments7,9,15 as a single quantitative organisation of composition space, obtained without auxiliary post-hoc attribution machinery. Three results support this picture.

(i) Architectural sign constraints (δLST ≥ 0, δtilt ≤ 0, confidence-gated δres) function as a structural inductive bias: they deliver calibrated conformal coverage and reduce OOD variance two- to four-fold relative to unconstrained baselines (Results, Table 1), without requiring explicit regularisers. The conformal layer turns the remaining residual variance into a distribution-free prediction interval.

(ii) The explicit branch decomposition recasts qualitative soft-mode and lone-pair arguments7,15 as quantitative per-composition attribution: δLST emerges as the largest single attributed contributor to permittivity in microwave-dielectric ABO3 ceramics, with the static-ionic CM baseline a near-uniform secondary contribution and tilt + residual essentially inactive (Results §1). We emphasise that δLST is the model's allocation of εr rather than a spectroscopically measured soft-mode amplitude: the model lacks phonon-frequency input, and independent confirmation would require external ωTO data. The non-negativity bound on δLST is slack throughout (δLST > 0.7), so the soft-mode share reflects a genuine model-attributed signal rather than an artefact of a flexible signed branch out-competing a fixed analytic baseline.

(iii) The A-site hierarchy Pb > Ca > La > Sr > Ba (Results §2; p < 10−3 under label permutation) emerges from the LST branch without being imposed — the sign constraint is identical across compositions, so the ranking is data-driven, not architectural. The monotonic Ba→Sr→La→Ca segment tracks Shannon 12-coordinate ionic-radius contraction; Pb breaks upward, probably reflecting 6s2 lone-pair stereoactivity15,16,26.

Two design inferences follow. First, for high-εr Pb-free microwave dielectrics, the optimal compositional zone the model identifies is the Sr-rich, d0-Ti/Zr corner of Reaney Regime III, with negligible tilt — exactly where the GA inverse-design optimum (Ba0.05Sr0.95Ti0.84Zr0.15O3, predicted εr ≈ 147, 90% LCB 132, fLST = 2.85) converges. This optimum lies in the sparse-data frontier flagged as an extrapolation by the applicability-domain density gate, and is reported as a confidence-bounded synthesis target rather than a validated material; the Pb-allowed run reaches predicted εr ≈ 166–170 but in a leave-Pb-out negative-R2 region and so cannot be read as a calibrated bound. Second, for ML extrapolation in this materials class, physics-aware confidence σconf reliably partitions compositions into chemically coherent applicability zones29: Pb in-AD = 74.4% (high confidence but LOFO R2 = −0.097, a confident-but-wrong failure mode that must be detected by mechanistic chemistry rather than by σ alone), versus Sr in-AD = 23.3% (low confidence, genuinely flagged as uncertain). Beyond Pb, Ba, the largest A-site family (n = 436), also fails to extrapolate from Ba-free data (LOFO R2 = 0.008), so the framework's reliable design zone currently excludes Ba-dominant compositions, a practically important caveat given their commercial prevalence. Reaney Regime Ia (LOFO R2 = −7.378) is similarly identified as a separate physical category, not just a tolerance-factor bin.

Two qualifications apply. First, the model predicts εr only; the quality factor Q×f and the temperature coefficient τf — the figures of merit any deployable microwave-dielectric resonator must satisfy jointly with high εr1,2 — are not predicted here. A 5G/6G base-station bandpass filter typically requires Q×f > 30,000 GHz and |τf| < 30 ppm K−1 in addition to a target εr; the Sr-rich, Ti-rich Regime III chemistry the model recommends is precisely the family whose τf and Q×f tradeoffs historically required compositional engineering — for instance, the end-member SrTiO3 has τ_f ≈ −1700 ppm K−1 at room temperature38, large negative values that have historically been compensated by d0 B-site substitutions (Zr4+, Sn4+) or layered-composite architectures, beyond the scope of this composition-only model. Synthesis-ready candidates should therefore be measured at 1–10 GHz using the cylindrical TE01δ dielectric-resonator (Hakki–Coleman) method39,40 to extract εr and Q×f, with τf swept over 25–85 °C; we report the proposed composition as a scientific target for such characterisation, not a drop-in 5G filter material. Second, the Sr-rich, Ca/Ce-substituted titanate chemistry the GA optimum lies adjacent to has been extensively measured in the microwave-dielectric literature and is well represented in our 1,304-composition training corpus (e.g., the (Sr,Ca)TiO31,38,41 and Sr1−3x/2CexTiO336 solid-solution series, spanning εr ≈ 113–185 over decades of measurement); the inverse-design contribution here is therefore not the chemical family itself, but a specific, physics-decomposed, conformal-bounded composition (Ba0.05Sr0.95Ti0.84Zr0.15O3) lying at the model's extrapolation frontier, together with the per-composition δLST attribution that identifies it as δLST-dominated rather than electronic.

Three limitations bound these claims. First, the decomposition is an interpretive attribution, not a measurement: because the model lacks access to phonon frequencies, δLST quantifies the lattice contribution the static-ionic baseline omits but stops short of independently measuring the soft-mode amplitude — external ωTO (e.g., FIR/THz spectroscopy36,42, hyper-Raman43, inelastic neutron scattering35,44) or first-principles validation on representative compositions10–12 would be required to close that gap, with recent systematic DFT calculations across 12 ABO3 perovskites10 and infrared-resolved phonon studies of the Sr-Ce-Ti microwave-ceramic family36 providing converging support for the soft-mode interpretation we attribute empirically at the corpus level. Such validation is itself non-trivial for these substitutionally disordered compositions, which fall outside existing high-throughput first-principles dielectric databases and require explicit supercell or special-quasirandom-structure treatment; first-principles characterisation of representative compositions is a natural next step. Internally, the hierarchy's structural invariance under 45 retrainings spanning ±50% perturbations of every σconf coefficient (Supplementary Fig. 24) separates empirical reproducibility (closed) from external phonon-frequency validation (open). The lattice contribution we name δLST is, in principle, a superposition of several channels: Born-charge enhancement, finite ionic polarizabilities beyond the Shannon tabulation5,22, electron-phonon coupling, dipolar disorder in solid solutions, and processing-induced extrinsic contributions. Each converges to the soft-mode amplitude in the displacive limit but can independently raise εr elsewhere. The single-channel assignment is therefore a coarse-grained attribution that brackets these mechanisms together, to be refined spectroscopically or from first principles. Second, the LST/tilt/residual partition is made identifiable by a strict disjoint feature assignment and a confidence-gated residual: under the disjoint-feature assumption and the bounded residual (\|δres\| ≤ s_res ≈ 48.2 multiplied by σconf ∈ [0,1]), the four-way decomposition is identifiable up to the residual mass that the gate admits, which the saturation defence (Results §1) shows is < 1% in aggregate. Formal global uniqueness guarantees are nevertheless lacking, and the tilt branch in particular is near-inactive (active for ~10% of compositions, −0.7% of εr) and should be read as a small, physically expected correction, not an independent predictor, consistent with recent evidence that octahedral tilting can be symmetry-decoupled from B-site off-centring. The Ba subset (n = 368 of the 1,124 valid-CM compositions) is dominated by 1:1 and 1:2 B-site-cation-ordered complex perovskites (Ba(B'B'')O3 workhorse microwave dielectrics45), in which the polar instability is frustrated by B-site order rather than by Ba A-site chemistry per se; the f_LST = 0.66 reported for Ba is therefore a corpus-composition statement (low εr in microwave-dielectric handbooks because of B-site ordering) rather than a statement about Ba's intrinsic soft-mode coupling, which in cubic BaTiO3 above T_c is, by contrast, among the softest in the perovskite family43,44 — first-principles calculations on appropriately-strained cubic BaTiO3 predict εs ≈ 7,300 via TO mode softening to ωTO ≈ 6 cm−111, two orders of magnitude above our handbook-Ba subset mean. Third, the model is composition-conditioned, processing and structural diversity (sintering, calcination, crystal system) enter only through engineered features, so within-composition variation from processing is absorbed as aleatoric uncertainty, not resolved. None of these undermines the central, physically anchored result: the A-site amplification hierarchy, which tracks ionic radius and Pb lone-pair chemistry independently of the constraint.

The architecture extends naturally beyond permittivity, in the lineage of additive interpretable models46 and physics-informed materials architectures47: a disjoint physics-feature partition with hard sign constraints and a confidence-gated residual is a template applicable wherever a parameter-free analytic baseline exists and the additive corrections carry physically meaningful signs, with ferroelectric Ps — decomposable into a King-Smith–Vanderbilt point-charge anchor22 plus signed Born-charge and anharmonic corrections — the most direct analogue. An analogous role of phonon softening has recently been quantitatively established for critical thermoelectric transport in Cu2Se-class materials37, where the same ω2 = b(Tp − T) soft-mode temperature dependence drives anomalies in both electrical resistivity and Seebeck coefficient through carrier–soft-TO-phonon interactions — confirming that the soft-mode framework δLST captures at the permittivity-corpus level applies more broadly to property classes whose microscopic mechanism is carrier–phonon coupling. The Pb "confident-but-wrong" failure (74.4% in-domain by σconf yet leave-Pb-out R2 = −0.097) is itself the manuscript's most transferable methodological lesson: in chemically isolated regions, mechanistic priors — not uncertainty magnitude alone — must gate extrapolation. The same warning extends directly to other ns2 lone-pair chemistries — Bi3+ in BiFeO3-class multiferroic perovskites, Sn2+ in lead-free halide perovskites and stannate ferroelectrics, In+ and Tl+ in chalcogenide thermoelectrics — where any applicability-domain criterion that is not informed by lone-pair-sensitive descriptors will exhibit the same failure mode. We note also that the d0 B-site requirement encoded in our soft-mode proxy (Methods eq. 4) is itself a perovskite-titanate-specific rule, and A-site-lone-pair-driven ferroelectrics with non-d0 B-sites (e.g., BiFeO3, where Fe3+ is d5) fall outside the proxy and would require an A-site-only soft-mode flag to bring into coverage.

We present a physics-constrained neural network that decomposes εr predictions for ABO3 ceramics into CM, LST, tilt and confidence-gated residual contributions. The model reaches R2 = 0.941 on a family-disjoint holdout (in-calibration conformal coverage 90.5% at nominal 90%; out-of-calibration bootstrap 89.9 ± 5.7%), reduces OOD variance 2–4× relative to unconstrained baselines, and statistically establishes the A-site amplification hierarchy Pb > Ca > La > Sr > Ba (permutation p < 10−3). Physics-constrained genetic-algorithm inverse design identifies one δLST-dominated lead-free composition (Ba0.05Sr0.95Ti0.84Zr0.15O3, predicted εr ≈ 147, 90% LCB 132) at the model's extrapolation frontier, reported as a confidence-bounded synthesis target awaiting εr, Q×f and τ_f characterisation. Together with the hierarchy's invariance under 45 retrainings under ±50% gate-coefficient perturbations (Supplementary Fig. 24) and convergence with recent first-principles, spectroscopic and neutron-scattering studies10–12,35–37, these results provide multi-axis support for the soft-mode interpretation.

# Methods

Dataset and features

The training corpus comprises 1,304 ABO3-type perovskite microwave-dielectric ceramic compositions — predominantly simple ABO3 perovskites plus ~11% ABO3-derived superstructures — with experimentally reported microwave-frequency permittivities, compiled from a handbook and ~200 primary literature sources (full source list in Supplementary References). The corpus was restricted to genuine perovskites by excluding ilmenite-structured ATiO3 phases (A = Mg, Zn, Co, Ni; tolerance factor t ≈ 0.8 or below; 6-coordinate octahedron rather than 12-coordinate perovskite cage), A-site-deficient defect phases (e.g. La1/3TaO3), and redundant duplicates. Of the cleaned 1,124 valid-CM compositions (procedure in Supplementary Note 1), 973 use an exact Shannon-polarizability CM and 151 double perovskites (A2BB′O6) use a virtual-crystal-approximation (VCA) CM; 180 compositions without a valid CM route through the no-CM fallback. Nominal compositions reported under different processing conditions are retained as physically distinct samples (1,304 entries span 894 distinct formulae; each row carries a unique feature vector). Distributions of measured εr, Reaney regime and A-/B-site occupancy are in Supplementary Figs. 1, 19 and 20.

Features are partitioned into three physics-motivated groups (103 inputs total): 30 LST features (ωTO/ωLO surrogates, soft-mode-related descriptors9), 30 tilt features (tolerance factor, octahedral-rotation descriptors, A-site electronegativity, Glazer-class proxies), and 43 residual features (composition-averaged elemental, electronic and ionic properties). The partition is strict (Supplementary Fig. 10). Train/calibration splitting uses Family-GroupShuffleSplit on the dominant A- and B-site cations, yielding 1,188 training and 116 calibration samples with zero family overlap (and zero formula overlap because the grouping variable is coarser than the formula); this split is fixed throughout. The calibration set is intentionally Regime-III-heavy (74/116 = 64%), providing OOD stress. Structure-property correlations across 12 descriptors are reported in Supplementary Fig. 21; δLST (Spearman ρ = +0.87) is the strongest single predictor, consistent with the largest aggregate SHAP attribution (Supplementary Fig. 11).

Physics formulations

The Clausius-Mossotti relation4,5 expresses the static permittivity of a polar dielectric in terms of the molar volume Vm and the sum of constituent ionic polarizabilities αi (Shannon polarizabilities4, recently extended to microwave-frequency materials48):

εr,CM = 3Vm + 8πiαi3Vm − 4πiαi	(1)

The Lyddane-Sachs-Teller relation6 links the static and high-frequency permittivities to the longitudinal and transverse optical phonon frequencies:

εsε∞ = ωLOωTO2	(2)

so that soft-mode softening (ωTO → 0) amplifies εs. Equivalently, the static permittivity decomposes microscopically into εs = ε∞ + (4π/Ω) Σm (Z_{m})^{2} / ω^{2}_{m} where Zm is the Born effective charge of mode m and Ω the unit-cell volume10–12,22; our additive decomposition εr = εr,CM + δLST + δtilt + δres (eq. 5) is the data-driven analogue at the composition level, with δLST carrying the lattice contribution the CM static-ionic baseline omits. The Goldschmidt tolerance factor13 governs the geometric stability of the perovskite cage:

t = rA + rO2 (rB + rO)	(3)

where rA, rB and rO are Shannon ionic radii49 in the appropriate coordination. The Reaney regimes3,14 partition tolerance-factor space into four classes governing the tilt geometry: Regime III for t ≤ 0.965 (antiphase + in-phase tilts); Regime II for 0.965 < t ≤ 0.985 (antiphase tilts); Regime Ib for t > 0.985 with soft-mode proxy True (incipient ferroelectric); and Regime Ia for t > 0.985 with soft-mode proxy False (paraelectric, untilted). The soft-mode proxy is True if and only if the B-site is d0 (Ti/Nb/Ta/Zr) and the A-site is polarizable (Ba/Sr/Pb/Bi) — a working heuristic introduced in this work, combining the d0 requirement for soft-mode-driven ferroelectricity15 with A-site polarizability16,26. (4)

PCNN architecture

The PCNN output is the additive decomposition

εr = εr,CM + δLST + δtilt + δres	(5)

where εr,CM is analytically evaluated from eq. (1) (parameter-free), and the correction branches are constrained as:

δLST = rregime · Softplus(hLST)	(6)

δtilt = −Softplus(htilt)	(7)

δres = σconf · tanh(hres) · sres	(8)

where rregime ∈ {1.0, 1.5, 0.9, 0.7} for Reaney regimes {Ia, Ib, II, III} is a fixed, non-learnable per-regime prior on the LST branch — initialised from Reaney regime taxonomy3 and held fixed throughout training and inference; sres ≈ 48.2 is a learned scale (initialised at 44.9); and σconf is a fixed, physics-based confidence gate:

σconf = sigmoid(β0 + β1capprox + β2gnorm + β3p)	(9)

with β = (−2.0, 3.0, 2.0, 2.0) chosen on physical priors before training and held fixed (non-learnable): β0 sets a low base activation; β1 on the binary VCA indicator capprox raises σconf for virtual-crystal-approximated baselines (151 of 1,124 valid-CM); β2 on gnorm (normalised global instability index) raises it on bond-valence-unstable structures; β3 on the binary phase descriptor p flags ambiguous-phase entries. The four β are not tuned on the 116-sample calibration set; under ±50% perturbation of each (9 perturbations × 5 seeds = 45 retrainings; Supplementary Fig. 24), the Pb > Ca > La > Sr > Ba hierarchy is preserved in every perturbation, with per-A-site fLST varying by ≤ 0.02 and holdout R2 in 0.929–0.937. The branch raw outputs are produced by feed-forward sub-networks operating on the 192-dimensional trunk representation concatenated with each branch's feature partition.

We define the soft-mode amplification factor

fLST = δLSTεr,CM	(10)

as the lattice contribution expressed as a multiple of the electronic baseline; it is the primary metric used for the A-site comparison in Results and for setting the LST capacity bound (below).

The shared trunk maps the 103 input features through four fully connected hidden layers (two central layers forming a residual block) to a 192-dimensional representation. Each branch sub-network concatenates this trunk output with its feature partition and applies a small feed-forward head with SiLU activations, LayerNorm per branch, and the output activations of eqs. (6)–(8); full per-layer widths are in Supplementary Table 6. For the ≈14% of compositions for which CM is undefined (mostly layered/homologous and untabulated-ion stoichiometries) a no-CM fallback MLP predicts εr directly. The PCNN forward pass, conformal calibration, inverse design and applicability-domain procedures are detailed in algorithmic form in Supplementary Note 3.

Training procedure

We optimise the network with AdamW50 (learning rate 1.107 × 10−3, weight decay 2.301 × 10−5, batch size 128, 500 epochs, early-stop patience 100). Mixup51 augmentation (α = 0.025) and stochastic weight averaging52 (engaged from epoch fraction 0.765 at SWA lr 2.513 × 10−5) give the final SWA weights. Training runs on a consumer laptop CPU in tens of minutes per seed (5-seed ensemble in under an hour); inference is sub-second per composition. The loss is

L = αlogLlog + 1 − αlog MSEεr, ε̂r + λLSTLLST + λGIILGII + λVCALVCA	(11)

with λLST = 1.484 × 10−3, λGII = 0.030, λVCA = 4.470 × 10−2 and log-loss weight αlog = 0.505. The three physics penalties have explicit forms:

LLST = ⟨ ReLU(δLST − 5 εr,CM)2 ⟩	(12)

LGII = ⟨ ReLU(εr,CM − ε̂r)2 𝕀GII<0.3 ⟩	(13)

LVCA = ⟨ δres2 capprox ⟩	(14)

LLST caps δLST at the LST capacity proxy (ωLO/ωTO)2 − 1; LGII penalises predictions below εr,CM for the 245 compositions with bond-valence GII < 0.353; LVCA suppresses δres on VCA rows. Hyperparameters were tuned by Optuna (100 trials, TPE sampler; Supplementary Table 1, convergence in Supplementary Fig. 3); λGII was re-tuned by post-hoc grid search after a GII data-loading correction. The reported model is a 5-seed ensemble (prediction = mean; across-seed std = σML, used in the GA fitness below; σconf is the separate physics-based gate of eq. (9), used also in the applicability domain).

Conformal prediction calibration

We use split conformal prediction28 to convert σconf into calibrated prediction intervals. The 116-sample family-disjoint set serves both as the calibration set and as the holdout on which R2 = 0.941 is reported — a known limitation of split conformal with small datasets, so the empirical coverage below is an in-calibration consistency check. The family-disjoint construction strictly violates the standard exchangeability assumption (the calibration set lives in families absent from training rather than i.i.d. with it); we therefore report a bootstrap-validated in-pool coverage and note that recent non-exchangeable conformal frameworks — weighted conformal under covariate shift54, conformal beyond exchangeability55, and f-divergence-robust validation56 — provide the theoretical machinery for true OOD coverage on a third held-out partition. To validate coverage out of calibration without sacrificing training data, we partitioned the 116-sample holdout 2,000 times into disjoint ≈77/39 calibration/coverage subsets, computed q̂ on the calibration subset and measured coverage on the disjoint subset; mean coverage matched nominal at 80.1 ± 7.7%, 85.4 ± 6.9%, 89.9 ± 5.7% and 95.0 ± 4.2% (nominal 80/85/90/95%). The 39-sample subset gives per-replicate SE ≈ 4.8% at 90%, so the 89.9 ± 5.7% range corresponds to a 95% bootstrap CI of roughly [84%, 96%]. The calibration set yields nonconformity scores si = |εr,i − ε̂r,i|; at nominal coverage 1 − α we compute

q̂1−α = Quantile{si}, ⌈(n + 1)(1 − α)⌉n	(15)

The prediction interval at composition x is

PIx = ε̂rx − q̂1−α, ε̂rx + q̂1−α	(16)

For α = 0.10 we obtain q̂90 = 14.38 εr units (band width 28.75 units, μ = +0.54). On this family-disjoint set the empirical coverage matches the nominal level to within 0.7 percentage points across all targeted levels (reported in full in the Results and Fig. 5b). The conformal bands are reported for every screened candidate composition in the discovery analysis.

Baseline comparison

We compared the PCNN against seven baselines on identical Strat-GSS 5-fold partitions and the same 116-sample holdout: CM-only (eq. 1, no learning), Ridge, Random Forest, XGBoost57, CatBoost58, a BPNN MLP (capacity matched to the PCNN trunk), and a PIRNN (output-only sign constraints, no branch decomposition or disjoint feature partition). All baselines share the same features, preprocessing and partitions; full hyperparameters are in Supplementary Table 5. Baseline HPs were held at literature-standard defaults rather than re-tuned with a matched 100-trial Optuna budget; matched-budget tuning would be expected to tighten point accuracy but not alter the OOD CV-variance ranking on which the architectural-bias claim rests (Results §4). Two flexible baselines (BPNN R2 = 0.957; PIRNN R2 = 0.937) match or exceed the PCNN's holdout R2 = 0.941; the PCNN's contribution is interpretable mechanism allocation with 2–4× lower OOD CV variance, not raw accuracy. Branch ablation (Fig. 4a) used a reduced 3-fold Strat-GSS × 3 seeds (full-PCNN R2 = 0.894 vs the full 0.893 ± 0.043, negligible fold-count bias). The 23 Shapley R2 decomposition over the 8 branch-presence coalitions was computed fold-paired (3 folds × 3 seeds): per fold/seed, the marginal contribution of a branch is the fold-R2 gain when it joins every other-branch coalition, averaged across the 9 fold/seed configurations, preserving the Shapley additivity axiom.

Leave-one-family-out generalisability test

A-site LOFO holds out every composition containing a given A-site cation, retrains, and evaluates: Ba (ntest = 436), Sr (180), Ca (421), La (125), Pb (86). Regime LOFO performs the parallel procedure for the four Reaney regimes (Ia, Ib, II, III). Statistical significance for the A-site and regime rank orderings is assessed by 2,000 permutation tests on the family-mean range. Hyperparameters are held fixed across LOFO folds at the values from the main Optuna search; refitting within each LOFO fold would risk per-fold tuning leakage, so the reported LOFO R2 represent transferability under a fixed-architecture deployment and constitute an upper bound on transfer failure (re-tuning could only improve held-out R2). The main Optuna search was conducted on the train+calibration partition with each LOFO-held-out family already excluded from inner CV folds, so no held-out-family information enters HP selection.

Applicability domain

The applicability domain is defined as the conjunction of two gates29,30. The physics gate flags a composition as in-domain iff σconf < 0.35 — using the same physics-based confidence gate σconf (eq. 9), here applied as a threshold criterion rather than as the δres multiplier of eq. (8) (735/1,304 = 56.4%). The density gate uses a Gaussian-kernel density estimator on the standardised 103-feature input30:

log p̂(x) = log1ntrainiKhx − xi	(17)

with bandwidth h selected by Scott's rule; a sample is flagged as in-domain iff log p̂(x) exceeds the 10th percentile of the training distribution (1,174/1,304 = 90.0%). The combined AD is the intersection (688/1,304 = 52.8% of the full corpus and 26.7% of the Regime-III-heavy holdout). Performance partitions accordingly: R2in = 0.933, R2out = 0.858 (gap 0.075). Per-A-site σconf is reported as Pb = 0.288, La = 0.298, Ba = 0.491, Ca = 0.509, Sr = 0.545, and the corresponding in-AD fractions are Pb = 74.4% (confident-but-wrong) and Sr = 23.3% (genuinely uncertain), illustrating the limits of σ-only OOD detection32,59,60.

Inverse design (genetic algorithm)

To search composition space directly rather than rank a fixed library, we used a physics-constrained genetic algorithm (GA)33,61 over the coupled A- and B-site composition simplices (A ∈ {Ba, Sr, Ca, La, Pb, Nd, Sm, Y, Bi, Ce}, B ∈ {Ti, Zr, Nb, Ta, Sn}). Three runs were performed: GA-Pb-allowed (full A-site), GA-Pb-free (Pb fraction = 0) and GA-d0-strict (B-site restricted to d0 cations {Ti, Zr, Nb, Ta}). Each run evolved a population of 100 individuals over 50 generations (≈ 5,000 PCNN forward evaluations) with tournament selection (k = 3), uniform crossover (rate 0.70), Gaussian composition mutation (rate 0.30, σ = 0.05 per cation), elitism (5 individuals) and 5% random immigration (seed 7). Charge balance is enforced by projection (|zA + zB − 6| ≤ 0.10), and candidates are rejected unless the Goldschmidt tolerance factor lies in [0.85, 1.05] and the d0 B-site fraction ≥ 0.5. The fitness maximises the ensemble-mean predicted εr penalised by predictive uncertainty, f = ε̂r − 0.5 σML (where σML is the ensemble standard deviation, distinct from the physics-gate σconf of the applicability domain); the GA therefore performs an uncertainty-penalised free search across the full composition simplices, with applicability-domain assessment applied post hoc to the resulting candidates rather than as a constraint during the search. Each reported candidate carries its 90% conformal interval (q̂90 = 14.38) and is assessed against the dual applicability domain (above) and its nearest-neighbour distance to the training set. Because each run converges to a single composition family per constraint set, we report the optimum per run rather than near-duplicate variants.

Statistics and reproducibility

All statistical tests were two-tailed. Statistical significance of the A-site amplification hierarchy was assessed by label-permutation tests (2,000 random permutations of A-site assignments; observed range 1.622 versus null mean 0.209; z ≈ 17σ; p < 0.0005); the regime ordering was tested identically (observed range 1.136; z ≈ 9σ; p < 0.0005). Conformal coverage out of calibration was validated by bootstrap (2,000 disjoint calibration/coverage partitions of the 116-sample family-disjoint holdout; mean coverage ± SD reported at nominal 80, 85, 90, 95% levels). Predictive uncertainty per prediction is the across-seed standard deviation of a 5-seed ensemble (σML), distinct from the physics-based confidence gate σconf of eq. (9); calibrated prediction intervals are split-conformal (eqs. 15–16). Spearman rank correlations are reported throughout with two-sided p-values. Error bars in figures denote either the 90% conformal prediction interval (Fig. 5a) or bootstrap 95% confidence intervals from 2,000 resamples (Fig. 2a); these are specified per figure caption. Exact sample sizes are reported as n in the text, in Tables 1–2 and in figure captions; no observations were excluded after the dataset-cleaning criteria described in Methods §Dataset and features. Software: model and training in PyTorch (≥ 2.0); hyperparameter search in Optuna (Tree-structured Parzen Estimator sampler, 100 trials); statistical tests and bootstrap in NumPy/SciPy. Random seeds, exact training schedule and the 5-seed ensemble identifiers are listed in Supplementary Table 1; the genetic-algorithm inverse-design uses seed 7.

# Data availability

The cleaned 1,304-composition ABO3 microwave-dielectric dataset, the 103-feature processed feature matrix, the fixed family-disjoint train/calibration partition, the per-sample additive-decomposition table (εr, εCM, δLST, δtilt, δres, σconf and σML for every composition), the per-figure source-data CSVs, and an accompanying spreadsheet enumerating the ~200 primary literature sources from which the experimental εr values were compiled have been deposited in Zenodo at https://doi.org/10.5281/zenodo.2043342762. Source data are provided with this paper.

# Code availability

The custom Python code used for dataset curation, feature engineering, PCNN architecture and training, conformal calibration, applicability-domain analysis, and physics-constrained genetic-algorithm inverse design has been deposited at GitHub https://github.com/anbu-nems/CMLTRPCNN, with an archival snapshot at Zenodo (concept DOI https://doi.org/10.5281/zenodo.20433402, resolving to the latest released version)63. The repository includes the scripts required to reproduce every analysis reported in this study together with the trained 5-seed ensemble checkpoint, a package manifest mapping each main display item to its reproduction script and result file (also reproduced in Supplementary Table 7), pinned dependency versions in `requirements.txt`, and usage instructions. The code is released under the MIT license.

# References

1. Reaney, I. M. & Iddles, D. Microwave dielectric ceramics for resonators and filters in mobile phone networks. J. Am. Ceram. Soc. 89, 2063–2072 (2006).

2. Sebastian, M. T. & Dixit, A. (eds). Microwave Materials and Applications (Wiley-IEEE Press, 2017).

3. Reaney, I. M., Colla, E. L. & Setter, N. Dielectric and structural characteristics of Ba- and Sr-based complex perovskites as a function of tolerance factor. Jpn. J. Appl. Phys. 33, 3984–3990 (1994).

4. Shannon, R. D. Dielectric polarizabilities of ions in oxides and fluorides. J. Appl. Phys. 73, 348–366 (1993).

5. Bosman, A. J. & Havinga, E. E. Temperature dependence of the dielectric constants of cubic ionic compounds. Phys. Rev. 129, 1593–1600 (1963).

6. Lyddane, R. H., Sachs, R. G. & Teller, E. On the polar vibrations of alkali halides. Phys. Rev. 59, 673–676 (1941).

7. Cochran, W. Crystal stability and the theory of ferroelectricity. Phys. Rev. Lett. 3, 412–414 (1959).

8. Cochran, W. Crystal stability and the theory of ferroelectricity. Adv. Phys. 9, 387–423 (1960).

9. Kim, K., Hwang, W., Oh, S.-H. V. & Soon, A. Exploring anharmonic lattice dynamics and dielectric relations in niobate perovskites from first-principles self-consistent phonon calculations. npj Comput. Mater. 9, 154 (2023).

10. Sophia, G., Baranek, P., Rérat, M. & Dovesi, R. The effect of composition on phonon softening in ABO3-type perovskites: DFT modelling. Phys. Chem. Chem. Phys. 24, 27064–27074 (2022).

11. Guo, H., Baker, J. S., Wu, W. & Choy, K. L. High dielectric constants in BaTiO3 due to phonon mode softening induced by lattice strains: First principles calculations. Adv. Phys. Res. 2, 2300001 (2023).

12. Cao, R. et al. Softening of the optical phonon by reduced interatomic bonding strength without depolarization. Nature 634, 1080–1085 (2024).

13. Bartel, C. J. et al. New tolerance factor to predict the stability of perovskite oxides and halides. Sci. Adv. 5, eaav0693 (2019).

14. Handley, C. M. et al. Dynamic tilting in perovskites. Acta Crystallogr. A 79, 163–170 (2023).

15. Cohen, R. E. Origin of ferroelectricity in perovskite oxides. Nature 358, 136–138 (1992).

16. Walsh, A., Payne, D. J., Egdell, R. G. & Watson, G. W. Stereochemistry of post-transition metal oxides: revision of the classical lone pair model. Chem. Soc. Rev. 40, 4455–4463 (2011).

17. Mao, Z., Li, W. & Tan, J. Dielectric tensor prediction for inorganic materials using latent information from preferred potential. npj Comput. Mater. 10, 265 (2024).

18. Xi, Z. et al. Active learning in latent spaces enables rapid inverse design of ferroelectric ceramics for energy storage. Nat. Commun. 17, 4281 (2026).

19. Li, W. et al. Generative learning facilitated discovery of high-entropy ceramic dielectrics for capacitive energy storage. Nat. Commun. 15, 4940 (2024).

20. Bajpai, A. et al. Attention-enhanced variational learning for physically informed discovery of exceptionally hard multicomponent bulk metallic glasses. Nat. Commun. 17, 4266 (2026).

21. Karniadakis, G. E. et al. Physics-informed machine learning. Nat. Rev. Phys. 3, 422–440 (2021).

22. Ghosez, P., Michenaud, J.-P. & Gonze, X. Dynamical atomic charges: the case of ABO3 compounds. Phys. Rev. B 58, 6224–6240 (1998).

23. Lines, M. E. & Glass, A. M. Principles and Applications of Ferroelectrics and Related Materials (Oxford University Press, 1977).

24. Lundberg, S. M. & Lee, S.-I. A unified approach to interpreting model predictions. Advances in Neural Information Processing Systems 30, 4765–4774 (2017).

25. Waghmare, U. V. & Rabe, K. M. Ab initio statistical mechanics of the ferroelectric phase transition in PbTiO3. Phys. Rev. B 55, 6161–6173 (1997).

26. Azuma, M. et al. Functional transition metal perovskite oxides with 6s2 lone pair activity stabilized by high-pressure synthesis. Annu. Rev. Mater. Res. 51, 329–349 (2021).

27. Sartor, D., Sinigaglia, A. & Susto, G. A. Advancing constrained monotonic neural networks: achieving universal approximation beyond bounded activations. Preprint at https://arxiv.org/abs/2505.02537 (2025).

28. Angelopoulos, A. N. & Bates, S. A gentle introduction to conformal prediction and distribution-free uncertainty quantification. Found. Trends Mach. Learn. 16, 494–591 (2023).

29. Sutton, C. et al. Identifying domains of applicability of machine learning models for materials science. Nat. Commun. 11, 4428 (2020).

30. Schultz, L. E., Wang, Y., Jacobs, R. & Morgan, D. A general approach for determining the applicability domain of machine learning models. npj Comput. Mater. 11, 95 (2025).

31. Li, K. et al. Probing out-of-distribution generalization in machine learning for materials. Commun. Mater. 6, 9 (2025).

32. Omee, S. S., Fu, N., Dong, R., Hu, M. & Hu, J. Structure-based out-of-distribution (OOD) materials property prediction: a benchmark study. npj Comput. Mater. 10, 144 (2024).

33. Eiben, A. E. & Smith, J. E. Introduction to Evolutionary Computing 2nd edn (Springer, 2015).

34. Hill, N. A. Why are there so few magnetic ferroelectrics? J. Phys. Chem. B 104, 6694–6709 (2000).

35. Zhang, Z. et al. Phonon lifetimes and mode softening in cubic Cs2AgBiBr6. Newton 1, 100097 (2025).

36. Moreira, R. L., Lobo, R. P. S. M., Subodh, G., Sebastian, M. T., Matinaga, F. M. & Dias, A. Optical phonon modes and dielectric behavior of Sr1−3x/2CexTiO3 microwave ceramics. Chem. Mater. 19, 6548–6554 (2007).

37. Zhao, K. et al. Modeling critical thermoelectric transports driven by band broadening and phonon softening. Nat. Commun. 15, 776 (2024).

38. Lemanov, V. V., Sotnikov, A. V., Smirnova, E. P., Weihnacht, M. & Kunze, R. Perovskite CaTiO3 as an incipient ferroelectric. Solid State Commun. 110, 611–614 (1999).

39. Hakki, B. W. & Coleman, P. D. A dielectric resonator method of measuring inductive capacities in the millimetre range. IRE Trans. Microw. Theory Tech. 8, 402–410 (1960).

40. Courtney, W. E. Analysis and evaluation of a method of measuring the complex permittivity and permeability of microwave insulators. IEEE Trans. Microw. Theory Tech. 18, 476–485 (1970).

41. Bednorz, J. G. & Müller, K. A. Sr1−xCaxTiO3: An XY quantum ferroelectric with transition to randomness. Phys. Rev. Lett. 52, 2289–2292 (1984).

42. Petzelt, J. et al. Dielectric, infrared, and Raman response of undoped SrTiO3 ceramics: evidence of polar grain boundaries. Phys. Rev. B 64, 184111 (2001).

43. Vogt, H. Refined treatment of the model of linearly coupled anharmonic oscillators and its application to the temperature dependence of the zone-centre soft mode in cubic BaTiO3. Phys. Rev. B 51, 8046–8059 (1995).

44. Harada, J., Axe, J. D. & Shirane, G. Neutron-scattering study of soft modes in cubic BaTiO3. Phys. Rev. B 4, 155–162 (1971).

45. Davies, P. K., Wu, H., Borisevich, A. Y., Molodetsky, I. E. & Farber, L. Crystal chemistry of complex perovskites: new cation-ordered dielectric oxides. Annu. Rev. Mater. Res. 38, 369–401 (2008).

46. Agarwal, R. et al. Neural additive models: interpretable machine learning with neural nets. In Advances in Neural Information Processing Systems 34, 4699–4711 (2021).

47. Zhao, W. et al. A physics-informed machine learning framework for accelerated discovery of single-phase B2 multi-principal element intermetallics. npj Comput. Mater. 11, 278 (2025).

48. Liu, J. et al. Optimizing and extending ion dielectric polarizability database for microwave frequencies using machine learning methods. npj Comput. Mater. 9, 178 (2023). _TODO_verify_article_number

49. Shannon, R. D. Revised effective ionic radii and systematic studies of interatomic distances in halides and chalcogenides. Acta Crystallogr. A 32, 751–767 (1976).

50. Loshchilov, I. & Hutter, F. Decoupled weight decay regularization. International Conference on Learning Representations (ICLR, 2019). arXiv:1711.05101.

51. Zhang, H., Cisse, M., Dauphin, Y. N. & Lopez-Paz, D. mixup: Beyond empirical risk minimization. International Conference on Learning Representations (ICLR, 2018). arXiv:1710.09412.

52. Izmailov, P., Podoprikhin, D., Garipov, T., Vetrov, D. & Wilson, A. G. Averaging weights leads to wider optima and better generalization. Uncertainty in Artificial Intelligence (UAI, 2018). arXiv:1803.05407.

53. Kato, H. et al. Complementary evaluation of structure stability of perovskite oxides using bond-valence and density-functional-theory calculations. Sci. Technol. Adv. Mater. 19, 155–161 (2018).

54. Tibshirani, R. J., Foygel Barber, R., Candès, E. J. & Ramdas, A. Conformal prediction under covariate shift. Advances in Neural Information Processing Systems 32, 2530–2540 (NeurIPS, 2019).

55. Barber, R. F., Candès, E. J., Ramdas, A. & Tibshirani, R. J. Conformal prediction beyond exchangeability. Ann. Stat. 51, 816–845 (2023).

56. Cauchois, M., Gupta, S., Ali, A. & Duchi, J. C. Robust validation: confident predictions even when distributions shift. J. Am. Stat. Assoc. (online, 2024). arXiv:2008.04267.

57. Chen, T. & Guestrin, C. XGBoost: a scalable tree boosting system. In Proc. 22nd ACM SIGKDD International Conference on Knowledge Discovery and Data Mining 785–794 (ACM, 2016).

58. Prokhorenkova, L., Gusev, G., Vorobev, A., Dorogush, A. V. & Gulin, A. CatBoost: unbiased boosting with categorical features. In Advances in Neural Information Processing Systems 31 (2018).

59. Segal, N., Netanyahu, A., Greenman, K. P., Agrawal, P. & Gómez-Bombarelli, R. Known unknowns: out-of-distribution property prediction in materials and molecules. npj Comput. Mater. 11, 345 (2025).

60. Panapitiya, G. & Saldanha, E. Outlier-based domain of applicability identification for materials property prediction models. Preprint at https://arxiv.org/abs/2302.06454 (2023).

61. Jennings, P. C., Lysgaard, S., Hummelshøj, J. S., Vegge, T. & Bligaard, T. Genetic algorithms for computational materials discovery accelerated by machine learning. npj Comput. Mater. 5, 46 (2019).

62. PCNN Authors. CMLTRPCNN — ABO3 microwave-dielectric permittivity dataset (n = 1,304). Zenodo https://doi.org/10.5281/zenodo.20433427 (2026).

63. PCNN Authors. CMLTRPCNN — physics-constrained neural network for ABO3 microwave-dielectric permittivity prediction (companion code release; concept DOI). Zenodo https://doi.org/10.5281/zenodo.20433402 (2026).

# Acknowledgements

The authors acknowledge [funding source 1] (grant [###]) and [funding source 2] (grant [###]) for financial support. Computational resources were provided by [computing facility]. We thank [colleagues, if any, for intellectual input not warranting authorship].

# Author contributions

[A.B.] conceived the project, designed the PCNN architecture, performed model training, cross-validation, applicability-domain analysis and inverse design, and wrote the manuscript. [C.D.] curated the dataset and the feature-engineering pipeline. [E.F.] supervised the work and contributed to interpretation. All authors discussed the results and approved the final manuscript. (CRediT taxonomy: insert specific role assignments — Conceptualization, Methodology, Software, Investigation, Formal analysis, Writing — original draft, Writing — review and editing, Visualization, Supervision, Funding acquisition.)

# Competing interests

The authors declare no competing interests.

# Materials & Correspondence

Correspondence and material requests should be addressed to [Corresponding Author Name] ([corresponding.author@institution.tld]).